# 10-Page Standard Operating Protocol: >99% Hemp-Monoculture Multiscale Vitrimer Composite

Document ID: SOP-HEMPOX-2026-v1.0 Organization: Hempoxies Division, Landry Industries, Moncton, NB, Canada Author: Marie-Soleil Seshat Landry Date: August 2026 Core Standard: ASTM D6866 / ISO 16620 (>99% Bio-based Carbon Content)

## SECTION 1: System Overview & Theoretical Framework

### 1.1 Executive Summary

This document provides the standard operating protocol for formulating, synthesizing, and processing a >99% hemp-derived multiscale vitrimer composite. The material system integrates an epoxidized and maleinized hempseed oil matrix cross-linked dynamically with a zinc catalyst, reinforced across five distinct spatial length scales using hemp-derived carbon and cellulose nanomaterials.

+---------------------------------------+
                     | BASE MATRIX (49 wt% EHO / 49 wt% MHO)  |
                     +-------------------+-------------------+
                                         |
                                         v
                     +---------------------------------------+
                     |    Zn(acac)2 DUAL CATALYST (2.0 wt%)  |
                     |   Dynamic Beta-Hydroxy Ester Exchange |[span_7](start_span)[span_7](end_span)
                     +-------------------+-------------------+
                                         |
        +--------------------------------+--------------------------------+
        |                                |                                |
        v                                v                                v
+---------------+                +---------------+                +---------------+
| MOLECULAR     |                | NANO-TIER     |                | MICRO / MACRO |
| 0.1-1 nm      |                | 1-100 nm      |                | um - mm       |
+---------------+                +---------------+                +---------------+
| Furfuryl      |                | HGO (0.3 phr) |                | Biochar       |
| Glycidyl Ether|      | HrGO (0.2 phr)|     | (4.0 phr)     |
| (8-12 phr)    |                | Nanosheets    |                | Short Carbon  |
+---------------+                | (0.7 phr)     |     | Fiber         |
                                 | CNC (1.5 phr) |                | (18 phr)      |
                                 +---------------+                +---------------+

### 1.2 Vitrimer Cross-Linking Mechanics

The network relies on the epoxide ring-opening reaction by cyclic anhydride groups, forming dynamic \beta-hydroxy ester linkages:

\text{Triglyceride-Oxirane} + \text{Triglyceride-Anhydride} \xrightarrow{\text{Zn(acac)}_2} \text{Triglyceride-}\beta\text{-hydroxy ester-Triglyceride}

In the presence of zinc acetylacetonate (\text{Zn(acac)}_2), these ester linkages undergo thermally activated transesterification exchange at elevated temperatures (180\text{--}200^\circ\text{C}), allowing stress relaxation (\tau^* < 300\text{ s}), full reprocessability, self-healing, and mechanical welding.

## SECTION 2: Material Specifications & Chemical Inventories

### 2.1 Reagent & Raw Material Specifications

| Component | Function / Role | Target Specification | Derivation Route | Source |
| --- | --- | --- | --- | --- |
| Epoxidized Hempseed Oil (EHO) | Base Epoxy Resin | Oxirane Oxygen: 7.0–7.5%; EEW: 220–230 g/eq | Cold-pressed hempseed oil + peracetic acid |  |
| Maleinized Hempseed Oil (MHO) | Anhydride Cross-linker | Acid Number: 100–110 mg KOH/g; Viscosity: <10 dPa·s | Hempseed oil + maleic anhydride (ene/Diels-Alder) |  |
| Furfuryl Glycidyl Ether (FGE) | Reactive Diluent / \pi\text{--}\pi Stacking | Vacuum Distilled (bp 80^\circ\text{C} at 1 mbar) | Hemp hemicellulose \rightarrow Furfural \rightarrow Glycidylation |  |
| Hemp Graphene Oxide (HGO) | Covalent Interfacial Nanofiller | C/O ratio: 2.0–2.5; XRD spacing: 0.8–1.0 nm | Modified Hummers oxidation of hemp biochar |  |
| Reduced Hemp GO (HrGO) | Electrical/Thermal Percolation | Thermal shock (1000^\circ\text{C}) or ascorbic acid | Reduction of HGO |  |
| Hemp Carbon Nanosheets | 2D High-Aspect Barrier | BET Surface Area: >1500\text{ m}^2/\text{g}; Thickness: 2–10 nm | KOH chemical activation (800^\circ\text{C}) of char |  |
| Cellulose Nanocrystals (CNC) | 1D Crack Pinning / Modulus | Length: 100–300 nm; Crystallinity: >80\% | Acid hydrolysis (64\text{ wt\% } \text{H}_2\text{SO}_4) of bast |  |
| Hemp Biochar | Micro 0D Interstitial Filler | Fixed Carbon: >70\text{ wt\%}; BET Area: >200\text{ m}^2/\text{g} | Slow pyrolysis (550^\circ\text{C}, \text{N}_2) of stalk |  |
| Short Hemp Carbon Fiber | Macro 1D Load Bearing | Length: 3–6 mm; Single-fiber strength: >1\text{ GPa} | Bast carbonization (1200^\circ\text{C}, Ar) + chopping |  |
| Anhydrous Ethanol | Dispersion Medium | Water content: <0.5\text{ wt\%} (Karl Fischer) | Hemp fermentation, distillation, 3\text{ Å} sieves |  |
| Zinc Acetylacetonate | Cure & Exchange Catalyst | Purity: >98\% (HPLC) | Chemical synthesis (Non-hemp origin, ~1.5 wt% total) |  |

## SECTION 3: Feedstock Derivation Procedures (SOP-001 through SOP-011)

### 3.1 SOP-EHO-001: Epoxidized Hempseed Oil Synthesis

- Charge 500 g cold-pressed hempseed oil and 150 g glacial acetic acid (30 wt% rel. to oil) into a 2 L three-neck round-bottom flask.

- Add 2.5 g concentrated \text{H}_2\text{SO}_4 (0.5 wt% rel. to oil) as catalyst.

- Heat contents to 40^\circ\text{C} with mechanical stirring at 400 rpm.

- Add 300 g \text{H}_2\text{O}_2 (30 wt% aqueous, 60 wt% rel. to oil) dropwise via a dropping funnel over 2 hours, keeping internal temperature at 40\text{--}50^\circ\text{C}.

- Elevate batch temperature to 70^\circ\text{C} and hold for 6 hours under continuous stirring.

- Cool to room temperature and transfer contents into a separatory funnel.

- Wash organic layer with warm deionized water (3 \times 200\text{ mL}) until aqueous discharge reaches \text{pH} > 5.

- Dry over 50 g anhydrous \text{Na}_2\text{SO}_4 for 2 hours, filter, and strip residual moisture/volatiles via rotary evaporation (60^\circ\text{C}, 20 mbar, 1 hour).

- Target Metrics: Oxirane oxygen 7.0\text{--}7.5\%; Epoxy Equivalent Weight (EEW) 220\text{--}230\text{ g/eq}. Yield: 520\text{--}540\text{ g}.

### 3.2 SOP-MHO-001: Maleinized Hempseed Oil Synthesis

- Charge 500 g filtered hempseed oil into a 1 L three-neck flask and purge with \text{N}_2 gas (99.999%) for 15 minutes.

- Add 100 g finely ground maleic anhydride (20 wt% rel. to oil).

- Heat to 100^\circ\text{C} with stirring at 300 rpm under constant \text{N}_2 purge.

- Maintain reaction at 100^\circ\text{C} for 4 hours.

- Cool system to 60^\circ\text{C} and strip any unreacted volatile species under vacuum.

- Target Metrics: Acid number 100\text{--}110\text{ mg KOH/g}; Viscosity <10\text{ dPa}\cdot\text{s} at 20^\circ\text{C}. Yield: 580\text{--}600\text{ g}.

### 3.3 SOP-FGE-001: Furfuryl Glycidyl Ether

- Furfural: React 200 g ground hemp stalks with 1\text{ L} of 3\text{ M }\text{H}_2\text{SO}_4 in a stainless steel autoclave at 180^\circ\text{C} for 30 min. Filter, extract liquid with toluene (3 \times 200\text{ mL}), and evaporate solvent. Yield: 30–35 g furfural.

- Furfuryl Alcohol: Combine 30 g furfural, 3 g Raney-Ni, and 100 mL ethanol in a Parr reactor. Pressurize with \text{H}_2 to 2 MPa and heat at 80^\circ\text{C} for 2 hours. Filter and evaporate ethanol. Yield: 28–30 g.

- Glycidylation: Mix 25 g furfuryl alcohol (0.255 mol) and 28.3 g epichlorohydrin (0.306 mol) at 0^\circ\text{C}. Add 20.4\text{ g} of 50 wt% NaOH dropwise over 1 hour. Warm to 50^\circ\text{C} for 4 hours. Extract with diethyl ether, wash with brine, dry over \text{MgSO}_4, and vacuum distill at 80^\circ\text{C} (1 mbar). Yield: 22–25 g.

### 3.4 SOP-HGO-001: Hemp-Derived Graphene Oxide

- Mix 90 mL \text{H}_2\text{SO}_4 and 10 mL \text{H}_3\text{PO}_4 (9:1\text{ v/v}) in an ice bath.

- Slowly add 1 g hemp biochar (<75\ \mu\text{m}) under constant magnetic stirring.

- Add 9 g \text{KMnO}_4 in small increments over 15 minutes to prevent exotherm spikes.

- Remove ice bath, heat to 50^\circ\text{C}, and maintain stirring for 12 hours.

- Quench reaction by pouring onto 200 g crushed ice containing 3\text{ mL} of 30\text{ wt\% }\text{H}_2\text{O}_2.

- Centrifuge (4000 rpm, 10 min) and wash sequentially with 1\text{ M HCl} (2 \times 100\text{ mL}) and deionized water until supernatant reaches \text{pH } 5\text{--}6.

- Dialyze against DI water for 3 days and freeze-dry at -50^\circ\text{C} (0.1 mbar) for 48 hours.

- Target Metrics: C/O ratio 2.0–2.5; XRD layer spacing 0.8–1.0 nm. Yield: 1.5–2.0 g.

### 3.5 SOP-HrGO-001: Hemp-Derived Reduced Graphene Oxide

- Method A (Thermal): Load 0.5 g HGO into a quartz boat inside a tube furnace. Purge with Argon (100 sccm) for 30 minutes. Rapidly heat to 1000^\circ\text{C} (20^\circ\text{C/min}), hold for 30 seconds, and cool under continuous Ar flow. Yield: 0.25–0.30 g.

- Method B (Chemical): Disperse 0.5 g HGO in 500 mL DI water via 30 min sonication. Add 2.0 g L-ascorbic acid, heat to 80^\circ\text{C}, and stir for 2 hours. Filter through a 0.22\ \mu\text{m} PVDF membrane, wash with ethanol/water, and dry at 60^\circ\text{C} under vacuum. Yield: 0.30–0.35 g.

### 3.6 SOP-HCNS-001: Hemp Carbon Nanosheets

- Mix 5 g ground biochar (<75\ \mu\text{m}) with 20 g KOH pellets (4:1\text{ w/w}) in a mortar using minimal ethanol to form a uniform paste. Dry at 80^\circ\text{C} overnight.

- Place mixture in a quartz boat within a tube furnace and purge with \text{N}_2 for 30 minutes.

- Ramp temperature to 800^\circ\text{C} (5^\circ\text{C/min}), hold for 1 hour under \text{N}_2 (100 sccm), and cool to room temperature.

- Wash product with 1\text{ M HCl} (200 mL) followed by DI water centrifugation until neutral \text{pH}. Dry at 120^\circ\text{C} under vacuum.

- Target Metrics: BET Surface Area >1500\text{ m}^2/\text{g}; Thickness 2–10 nm. Yield: 3.0–3.5 g.

### 3.7 SOP-CNC-001: Cellulose Nanocrystals from Hemp Bast

- Alkaline Pulping: Treat 50 g dew-retted hemp bast fibers in 1\text{ L} of 2\text{ M NaOH} at 80^\circ\text{C} for 2 hours. Filter and wash to neutral \text{pH}.

- Bleaching: Suspend 30 g alkali cellulose in 500 mL water with 6 g \text{NaClO}_2 and acetic acid (\text{pH } 4.5\text{--}5.0) at 80^\circ\text{C} for 1 hour. Filter, wash, and dry.

- Acid Hydrolysis: Cool 300\text{ mL} of 64\text{ wt\% }\text{H}_2\text{SO}_4 to 45^\circ\text{C}. Add 20 g bleached cellulose under high-shear stirring and maintain at 45^\circ\text{C} for 45 minutes.

- Quench reaction with 3\text{ L} ice-cold DI water. Centrifuge (10,000\text{ rpm}, 10 min) repeatedly to eliminate acidic supernatant. Dialyze against DI water until neutral, concentrate via rotary evaporation, and spray-dry.

- Target Metrics: Length 100–300 nm; Diameter 5–20 nm; Crystallinity >80\%. Yield: 8–10 g.

### 3.8 SOP-BIO-001: Hemp Biochar Production

- Load 500 g air-dried, chopped hemp stalks (2\text{--}5\text{ cm}) into a stainless steel retort.

- Purge system with \text{N}_2 (100 sccm) for 30 minutes.

- Ramp furnace temperature to 550^\circ\text{C} (5^\circ\text{C/min}) and hold for 2 hours.

- Cool under nitrogen atmosphere to ambient room temperature.

- Ball-mill solid pyrolyzate to pass a <250\ \mu\text{m} sieve.

- Target Metrics: Fixed carbon >70\text{ wt\%}; BET surface area >200\text{ m}^2/\text{g}. Yield: 125–150 g.

### 3.9 SOP-SCF-001: Short Hemp Carbon Fiber

- Align 50 g dew-retted hemp bast fibers inside a quartz boat.

- Insert into tube furnace and purge with Argon for 30 minutes.

- Heat to 1200^\circ\text{C} (5^\circ\text{C/min}), maintain target for 2 hours under Ar flow, and cool down.

- Precision-chop carbonized strands into 3\text{--}6\text{ mm} lengths.

- Sieve through fine mesh screens to eliminate dust and particulate fraction (<1\text{ mm}).

- Target Metrics: Tensile strength >1\text{ GPa}. Yield: 10–13 g.

### 3.10 SOP-ETOH-001: Anhydrous Ethanol Dispersion Solvent

- Pretreatment: Autoclave 500 g ground stalks in 2\text{ L} of 1\text{ wt\% }\text{H}_2\text{SO}_4 at 121^\circ\text{C} for 30 min. Neutralize to \text{pH } 4.8 using \text{Ca(OH)}_2.

- Enzymatic Hydrolysis: Add cellulase enzyme cocktail (15\text{ FPU/g glucan}) in citrate buffer (\text{pH } 4.8, 2 L). Incubate at 50^\circ\text{C}, 150 rpm for 72 hours.

- Fermentation: Inoculate hydrolysate liquid with Saccharomyces cerevisiae (0.5\text{ g/L}). Ferment at 30^\circ\text{C} for 48 hours.

- Distillation & Dehydration: Distill at 78^\circ\text{C} to recover 95 wt% ethanol. Pass distillate through a packed column of pre-dried 3\text{ Å} molecular sieves at 25^\circ\text{C} (residence time: 30 min).

- Target Metrics: Moisture <0.5\text{ wt\%} via Karl Fischer titration. Yield: 25–35 g.

### 3.11 SOP-CAT-001: Zinc Acetylacetonate Catalyst

- Dissolve 10 g \text{Zn(NO}_3\text{)}_2\cdot 6\text{H}_2\text{O} in 50\text{ mL} DI water.

- Add 12\text{ mL} acetylacetone dropwise under continuous stirring.

- Adjust solution \text{pH} to 7–8 using 2\text{ M NaOH} to precipitate product.

- Stir suspension for 1 hour, filter, wash with ethanol (3 \times 50\text{ mL}) and water (2 \times 50\text{ mL}).

- Vacuum-dry at 80^\circ\text{C} overnight. Recrystallize from hot ethanol if purity <98\%. Yield: 8–9 g.

## SECTION 4: Standard Baseline Formulation Table

| Tier | Component | Specific Loading | Functional Role |
| --- | --- | --- | --- |
| Matrix Base | Epoxidized Hempseed Oil (EHO) | 49.0 wt% | Epoxide Matrix Monomer |
| Matrix Base | Maleinized Hempseed Oil (MHO) | 49.0 wt% | Anhydride Cross-linking Agent |
| Matrix Base | Zinc Acetylacetonate | 2.0 wt% | Cure Accelerator & Dynamic Exchange Catalyst |
| Molecular Scale | Furfuryl Glycidyl Ether (FGE) | 8–12 phr | Viscosity Reduction; Filler Interfacial \pi\text{--}\pi Stacking |
| Nano 2D Scale | Hemp-Derived GO (HGO) | 0.3–0.5 phr | Interfacial Covalent Coupling & Crack Deflection |
| Nano 2D Scale | Hemp-Derived rGO (HrGO) | 0.2–0.3 phr | Electrical/Thermal Percolation Network |
| Nano 2D Scale | Hemp Carbon Nanosheets | 0.5–1.0 phr | Gas/Moisture Barrier; High Aspect Ratio Stiffness |
| Nano 1D Scale | Cellulose Nanocrystals (CNC) | 1.0–2.0 phr | Rod-like Crack Pinning & Intersegmental Modulus |
| Micro 0D Scale | Hemp Biochar | 3.0–5.0 phr | Interstitial Micro-filler & Compressive Support |
| Macro 1D Scale | Short Hemp Carbon Fiber | 15–20 phr | Primary Structural Load-Bearing Reinforcement |
| Processing Aid | Anhydrous Hemp Ethanol | 50–100 phr | Solvent Medium for Nanofiller Dispersion (Stripped) |

Note: Parts per hundred resin (phr) values calculated relative to combined EHO + MHO mass.

## SECTION 5: Master Processing & Curing Protocol

[Phase 1: Solvent Dispersion] 
    |-- Bath Sonicate (30 min) HGO/HrGO/Nanosheets/CNC in Anhydrous Ethanol
    |-- Probe Sonicate (10 min, 30% amplitude)
    +-- Add Micro Biochar --> Bath Sonicate (10 min)
            |
            v
[Phase 2: Desolvation & Milling]
    |-- Rotary Evaporate Solvent (60 deg C, 50 mbar)
    |-- Vacuum Oven Drying (80 deg C, 12 hours)
    +-- Blend Dry Filler Paste with EHO + FGE via Three-Roll Mill (3000 rpm, 10 min)
            |
            v
[Phase 3: Activation & Integration]
    |-- Incorporate MHO and Zn(acac)2 Catalyst
    |-- Degas Under Vacuum (80 deg C, 30 min, <5 mbar)
    +-- Fold in Short Carbon Fibers via Planetary Mixer (Low Speed)
            |
            v
[Phase 4: Stepped Thermal Cure Cycle]
    |-- 120 deg C for 2 Hours (Gelation & Initial Network Formation)
    |-- 150 deg C for 2 Hours (Advanced Cross-linking)
    +-- 180 deg C for 2 Hours (Post-Cure Density Optimization)

## SECTION 6: Network Preservation & Catalyst Compensation Rules

### 6.1 Catalyst Surface Adsorption Rules

Oxygenated functional groups on HGO and HrGO surfaces adsorb \text{Zn}^{2+} coordination sites, starving the vitrimer matrix of active transesterification centers.

\text{Catalyst Compensation Rule: If Total Nanofiller Loading } > 2.0\text{ phr}, \text{ Increase }\text{Zn(acac)}_2 \text{ to } 2.5\text{--}3.0\text{ phr}

Alternatively, pre-passivate HGO/HrGO surfaces by stirring nanofillers in a 0.5 wt% \text{Zn(acac)}_2 ethanol solution for 1 hour prior to primary resin blending.

### 6.2 Stress Relaxation Protocol

Every production batch must pass Stress Relaxation Rheology to verify dynamic network preservation:

- Instrument Parameter: Parallel plate rheometer (25\text{ mm} plate, 1.0 mm gap).

- Test Conditions: Constant shear strain \gamma = 1.0\%, temperature T = 180^\circ\text{C}.

- Acceptance Criterion: Normalized relaxation modulus must decay below 1/e (\approx 37\%) within \tau^* < 300\text{ seconds}.

## SECTION 7: Material Property Tuning & Sensitivity Analysis

### 7.1 Stoichiometric Sensitivity

- Anhydride Excess (\text{MHO:EHO} = 55:45\text{ wt\%}): Increases cross-link density, pushing T_g up to 100\text{--}115^\circ\text{C}. Increases \tau^* to >600\text{ s} at 180^\circ\text{C}, degrading thermal reprocessability.

- Epoxide Excess (\text{EHO:MHO} = 55:45\text{ wt\%}): Lowers T_g to 60\text{--}75^\circ\text{C}, increases elongation at break (>15\%), and reduces uncured resin viscosity to improve fiber wetting.

### 7.2 FGE Rheological & Dynamic Tuning

- <8\text{ phr FGE}: Uncured viscosity remains high (>5000\text{ mPa}\cdot\text{s} at 80^\circ\text{C}), preventing complete fiber wet-out.

- 8\text{--}12\text{ phr FGE}: Drops viscosity to 2000\text{--}3000\text{ mPa}\cdot\text{s}, increases nanofiller dispersion by 30–50% via furan \pi\text{--}\pi stacking, and accelerates stress relaxation.

- >12\text{ phr FGE}: Reduces network density, dropping T_g by 10\text{--}20^\circ\text{C} and causing thermal-oxidative instability above 200^\circ\text{C}.

### 7.3 HGO:HrGO Electrical Percolation Switch

- HGO Only (0.5 phr): Electrical conductivity < 10^{-8}\text{ S/cm} (Insulator).

- HrGO Only (0.5 phr): Electrical conductivity 10^{-4}\text{--}10^{-2}\text{ S/cm} (Semiconductor), but degrades tensile strength by 10–15% due to filler agglomeration.

- Hybrid (2:1 to 3:1 HGO:HrGO): Achieves conductive percolation (10^{-3}\text{--}10^{-1}\text{ S/cm}) while retaining 90% of maximum mechanical strength.

## SECTION 8: Application-Specific Testing Variants (Variants 1 through 8)

The table below summarizes eight engineered formulations designed to meet or exceed specific properties of common engineering materials.

| Variant ID | Target Incumbent | Key Formulation Changes | Target Performance Metrics | Test Protocol Standard |
| --- | --- | --- | --- | --- |
| HEMP-AL | Aluminum 6061-T6 | MHO 55 wt%; 25 phr aligned short carbon fiber; 2.5 phr catalyst | \rho = 1.35\text{ g/cm}^3; E = 38\text{ GPa}; Specific Modulus = 28.1\text{ GPa}\cdot\text{cm}^3/\text{g} (+9.8% vs. Al) | ASTM D3039 / ASTM D6641 |
| HEMP-STEEL | Mild Steel | MHO 52 wt%; 22 phr random-in-plane carbon fiber; 4 phr biochar | \rho = 1.32\text{ g/cm}^3; \sigma_{\text{tensile}} = 220\text{ MPa}; Specific Strength = 167\text{ MPa}\cdot\text{cm}^3/\text{g} (+193% vs. Steel) | ASTM D3039 / ASTM D6110 |
| HEMP-PLAST | ABS Plastic | EHO 55 wt%; 12 phr FGE; 8 phr biochar; 10 phr carbon fiber | \rho = 1.18\text{ g/cm}^3; \sigma = 85\text{ MPa}; E = 5.5\text{ GPa}; Elongation at break \approx 12\% | ASTM D638 / ASTM D256 |
| HEMP-CRETE | C30 Concrete | 15 phr fine biochar + 30 phr coarse biochar (1–3 mm aggregate); 12 phr fiber | \rho = 1.45\text{ g/cm}^3; \sigma_{\text{compressive}} = 55\text{ MPa} (+83%); \sigma_{\text{tensile}} = 35\text{ MPa} (+1067%) | ASTM C39 / ASTM C496 |
| HEP-OXY | Petroleum DGEBA Epoxy | EHO:MHO 49:49 stoichiometric; 15 phr carbon fiber; 1.5 phr CNC | \rho = 1.28\text{ g/cm}^3; \sigma = 140\text{ MPa}; E = 12\text{ GPa}; Fully reprocessable | ASTM D3039 / ASTM D5868 |
| HEMP-KEV | Kevlar-49 | MHO 60 wt%; 30 phr aligned short carbon fiber; 2 phr CNC | \rho = 1.42\text{ g/cm}^3; \sigma_{\text{tensile}} = 420\text{ MPa}; E = 52\text{ GPa}; Omnidirectional impact toughness | ASTM D3039 / NIJ Level IIA |
| HEMP-TITAN | Ti-6Al-4V Titanium | MHO 55 wt%; 28 phr aligned fiber; 3.6 phr total nanofillers | \rho = 1.38\text{ g/cm}^3; E = 42\text{ GPa}; Specific Modulus = 30.4\text{ GPa}\cdot\text{cm}^3/\text{g} (+18% vs. Ti) | ASTM D3039 / ASTM E831 |
| HEMP-GFRP | E-Glass / Epoxy | MHO 52 wt%; 20 phr random-in-plane carbon fiber; 1.5 phr CNC | \rho = 1.30\text{ g/cm}^3; \sigma = 200\text{ MPa}; E = 26\text{ GPa}; Reprocessable, 28% lighter | ASTM D3039 / ASTM D2344 |

## SECTION 9: Thermal Reprocessing & Circularity Protocols

### 9.1 Compression Molding Reprocessing (Recycling) Protocol

- Granulate cured vitrimer scrap into fine particles (1\text{--}3\text{ mm}) using a mechanical composite grinder.

- Load granulated scrap into a matched metal compression mold pre-heated to 180^\circ\text{C}.

- Apply 3.0 MPa pressure for 20 minutes to allow dynamic \beta-hydroxy ester transesterification bond exchange across granule boundaries.

- Cool mold under pressure to <60^\circ\text{C} before demolding.

### 9.2 Lap-Shear Thermal Welding Protocol

- Surface-clean two cured vitrimer composite plaques using anhydrous hemp ethanol.

- Overlap plaque ends by 12.5\text{ mm} inside a heated lap-shear welding fixture.

- Clamp joint at 2.0 MPa pressure and heat joint interface to 190^\circ\text{C} for 15 minutes.

- Cool under pressure. Joint strength must exceed 90% of monolithic lap-shear strength when evaluated under ASTM D5868.

## SECTION 10: Quality Control, ASTM Standards & Safety Data

### 10.1 Quality Control Test Matrix

+----------------------------------+
                      |   BATCH QUALITY CONTROL MATRIX   |
                      +----------------+-----------------+
                                       |
        +------------------------------+------------------------------+
        |                              |                              |
        v                              v                              v
+---------------+              +---------------+              +---------------+
| CHEMICAL QC   |              | PHYSICAL QC   |              | RHEOLOGY QC   |
+---------------+              +---------------+              +---------------+
| Oxirane Oxygen|    | Archimedes    |              | Stress        |
| (AOCS Cd 9-57)|              | Density       |   | Relaxation    |
| Acid Number   |    | (ASTM D792)   |              | (180 deg C)   |
| (ASTM D6641)  |              | Void Content  |   | tau* < 300 s  |
+---------------+              | (ASTM D2734)  |              +---------------+
                               +---------------+

### 10.2 Bio-Based Carbon Verification Standard

Pursuant to ASTM D6866 / ISO 16620 radiocarbon (^{14}\text{C}) testing, all matrix monomers and carbon nanofillers qualify as 100% modern biological carbon. The non-renewable mass fraction is limited to \approx 1.5\text{ wt\%}, originating exclusively from the zinc acetylacetonate catalyst core.

### 10.3 Laboratory Safety & Handling

- Nanofiller Handling: Handle dry HGO, HrGO, nanosheets, and CNC inside a HEPA-filtered ISO Class 5 laminar flow hood with certified N95 or P100 respirator protection to avoid inhalation risks.

- Thermal Hazards: High-temperature processing (180\text{--}200^\circ\text{C}) during curing and vitrimer thermoforming requires heat-resistant Kevlar gloves and face protection.